## Slide 1: Progress Report: Development of a Visible-NIR Photoluminescence Microspectrometer
Zach Colbert
Department of Physics, OSU
Advisor: Matt Graham
13 November 2018

## Slide 2: Goals
Couple laser light source into microscope
Couple PL light into Ocean Optics with fiber
Measure visible PL, compare to other data
Couple PL light into InGaAs CCD with grating
Measure NIR PL, compare to other data
Write detailed SOP for taking measurements
(Optional) Measure new materials

## Slide 3: Photoluminescence
Excitation (Single wavelength)
  Absorb photon
  Electron to “excited state” (“bound state”?)
Relaxation
  Lose energy to vibration
  Electron to slightly lower “vibronic state”
Shinde, K. N., et al (2012). Basic Mechanisms of Photoluminescence. Phosphate Phosphors for Solid-State Lighting (pp.41-59). Berlin: Springer.

## Slide 4: Photoluminescence
Emission (Spectral)
  “Radiative relaxation”
  Lose energy to photon emission
  Electron back to ground state
Measurement
  Spectrum of emission
  Intensity of emission

## Slide 5: Detectors
Not universally sensitive to all wavelengths
Visible Range (400-700 nm)
  Si sensors commonly used
  Easy application: Ocean Optics spectrometer
Near-Infrared (NIR) Range (800-2500 nm)
  InGaAs sensors commonly used
  Challenge: Grating, linear CCD

## Slide 6: Configuration for Visible PL
Completed summer 2018
Excites with 405nm laser diode
Fiber-coupled Ocean Optics spectrometer
Early results compared to measurements on existing system look good

## Slide 7: Configuration for Visible PL

## Slide 8: Configuration for Visible PL

## Slide 9: Poster

## Slide 10: Next Steps
Literature Review – Winter Break
  Optics: How do reflective gratings work?
  Optics: How to rigorously align light from grating to InGaAs array CCD?
  Works using similar systems
Optical Design and Setup – End of Break
NIR Measurements – Winter Break
Comparison and Analysis – Winter Break